Novel ElectrospunBio-MOF / Polyaniline Nanocomposite for Flammable Gas Detection

H. Shokry Hassan1,2, a \*,M.F.Elkady3,4, b,Kamal E. Diab1,c, Saad Mahmoud5,d, Raya Al-Dadah5,e

1aEnvironmental Engineering Department, Egypt-Japan University of Science and Technology, New Borg El‑Arab City, Alexandria, Egypt

2Electronic Materials Researches Department, Advanced Technology and New Materials Research Institute, City of Scientific Research and Technological Applications (SRTA-City), New Borg El-Arab, 21934, Alexandria, Egypt

3Chemical and Petrochemical Engineering Department, Egypt-Japan University of Science and Technology, New Borg El-Arab, Alexandria, Egypt

4Fabrication Technology Researches Department, Advanced Technology and New Materials Research Institute, City of Scientific Research and Technological Applications (SRTA-City), New Borg El-Arab, 21934, Alexandria, Egypt

5 Department of Mechanical Engineering, University of Birmingham, Edgbaston, Birmingham B152TT, UK

[ahassan.shokry@ejust.edu.eg](mailto:ahassan.shokry@ejust.edu.eg),[bmarwa.elkady@ejust.edu.eg](mailto:bmarwa.elkady@ejust.edu.eg), c[kamalediab1@gmail.com](mailto:kamalediab1@gmail.com), dS.M.MAHMOUD@bham.ac.uke[R.K.AL-DADAH@bham.ac.uk](mailto:R.K.AL-DADAH@bham.ac.uk),

**Keywords:**polyaniline; nanofiber; gas detector; Flammable Gas;electrospinning.

**Abstract.**Novel polyaniline (PANI)/bio-MOF hybrid nanomaterials were prepared successfully via sol-gel technique onto the polymerization process of PANI. The most proper synthetic nanohybrid was characterized using SEM, XRD, FTIR, and TGA. The optimum ratio was recorded using the first route to be 1 PANI: 1.5 Zr. The synthetic nanohybrid showed a crystalline structure with nanotube branching (like cauliflower) morphology. Electrospinning technique was used to fabricate a composite nanofiber matrix using polyvinyl alcohol (PVA) with the optimum prepared PANI/Zr nanocomposite. Electrospinning parameters including flow rate, collecting distance, and applied voltage were optimized to attain uniform composite nanofibers. The gas sensitivity of the synthetic nanofiber composite towards liquefied petroleum gas (LPG) as a function of temperature was specified by measuring the conductivity of two sputtered electrodes ofthe sensor’s devices. The nanofiber matrix showed the highest sensing performance for LPG within 10 sec at 200 ℃.

**Acknowledgments**

This work was supported by The British Council under Research Environment Links call for project entitled "Capacity Building in Egypt for Enhancing water availability, food security and renewable energy using MOF adsorption heat pumps” (Grants no. 871105921).